## Slide 1: Emergent phenomena at oxide interfaces
Chen Ke, Liu Donghao, Lv Peng, Shen Bingran,
Yan Qirui, Yang Wuhao, Ye Qijun, Zhu Chenji
Nov. 19th

## Slide 2: Outline
Basics
  Transition metal oxides and its interface
  Interacting electrons and magnetism
  Charge, orbital and spin reconstructions
Application
  Interface superconductivity
  Fractional quantum Hall effect

## Slide 3: The periodic table

## Slide 4: Electronic structure of TM
The d electrons play the domain role in TMOs properties

## Slide 5: Perovskite structure of TMOs
A: rare earth or alkaline earth elements
M: transition metal
O: oxide

## Slide 6: A fundamental understanding
the symmetry of the order parameter
Symmetry change leads to phase transition
  Spatial inversion (I)
  Time-reversal (T)
  Gauge (G)
  Spontaneous electric polarization
  Magnetism
  Superconductivity or super fluidity
Break
Notes: the ordered phase has lower symmetry than the Hamiltonian of the system

## Slide 7: Hubbard model
Interaction Hamilton
Approximation of short-range Coulomb interaction
The simplest many-particle model

## Slide 8: Hopping process
e_g
t_2g

## Slide 9: Relativistic effects

## Slide 10: Charge transfer
CaMnO_3
CaRuO_3
Antiferromagnetic
insulator
Paramagnetic
metal
heterointerface
ferromagnetic

## Slide 11: Electrostatic boundary conditions
Polar catastrophe

## Slide 12: Interface superconductivity
LaAlO3/SrTiO3 heterostructure

## Slide 13: Spin & orbital reconstructions
With charge transfer
With the mismatch of lattice parameter
With the local structure differing from bulk

## Slide 14: Various device structure
Phys. Rev. Lett. 103, 226802 (2009).
Nature Mater. 7, 855–858 (2008).
Nature 462, 487–490 (2009).

## Slide 15: Response to external field
Phys. Rev. Lett. 103, 226802 (2009).
Nature Mater. 7, 855–858 (2008).

## Slide 16: δ-doping SrTiO3 Nature 462, 487–490 (2009).
Dopant-layer thickness below the other character length
Free from large electronic disorder, high quality
High mobility
Shubnikov–deHaas oscillations in normal state

## Slide 17: Sample structure and transport characterization
b, Low-field sheet carrier density, Ns (red), and electron Hall mobility, m (blue), versus temperature.
c, Sheet resistance, rxx, versus temperature, showing a clear superconducting transition at 370 mK.

## Slide 18: Two-dimensional superconducting characteristics
a, Measurement of superconducting upper critical field, Hc2, using resistance versus magnetic field, H, for various angles between the sample plane and the magnetic field at T=50 mK. Rn, normal-state resistance.

## Slide 19: Two-dimensional superconducting characteristics

## Slide 20: Shubnikov-de Haas oscillations
The SdH oscillations are oscillations of the resistivity parallel to the current flow in the edge states of a 2DEG in an applied magnetic field.
related to the Quantum-Hall effect and share the same 1/B-periodicity.
Effective tool to investigate electronic structure

## Slide 21
Fractional quantum Hall effect in ZnO/(MgZn)O heterostructures

## Slide 22: Experiments
Science 315, 1388–1391 (2007).
Phys. Rev. B 84, 033304 (2011).

## Slide 23
Nature Mater. 9, 889–893 (2010).

## Slide 24
TMO interface is where new phenomenon merge
Possibility of combining these new phenomenon with theversatile functionality of the highly tunable metal oxide devices
Helpful for understanding some of the frontier of physics such as high superconductor
“The interface is the device”, stated Herbert Kroemer in his Nobel address.
Summary